Refinement method: Use GSAS2 directly, with the 3 phases (Mo Im3m, Mo2C ortho, MoC cubic), and systematically use these steps for refinement:

- Background — set to 3 terms, check refinement box → Refine

- Add zero shift → Refine

- Add phase fractions for the 3 phases → Refine

Objective function: phase composition, sigma (only request phase composition from the model --- side thought: should we consider feeding model its prediction and uncertainties vs the labels)

Trajectory 1: Use all initial Mo-Sucrose points above 450 C in BOICL loop

Trajectory 2: Use two initial points, one being the new M14 (I ran) and one of the points with the cubic phase present, which Eva ran.

SOPs:

- SOP: Cubic Mo/Sucrose Synthesis-1

In a beaker, 1 g of ammonium heptamolybdate tetrahydrate and 565.5 mg of sucrose is

dissolved in 7.07 mL of DI water. This solution is stirred for 15 minutes at 300 RPM, after which it is dried at 120 °C in air for 24 hours. After drying, the material is crushed in a mortar and pestle. To carburize the sample, 1 g of crushed and dried material is added to a crucible. The sample is heated at a ramp rate of 10 °C/min to a hold temperature of ___ °C for ____ hr under 100 ccm of ___ gas. After carburization, the sample is cooled under 30 ccm of N2 gas until the tube furnace reads below 30 °C. The sample is passivated under 30 ccm of 1% O2/N2 gas for 2 hours.

- SOP: Cubic Mo/Sucrose Synthesis-2

In the first beaker, 1 g of ammonium heptamolybdate tetrahydrate is dissolved in 6 mL of DI water. In the second beaker, 1 g of sucrose is dissolved in 1.5 mL of DI water. The sucrose solution in the second beaker is poured into the metal precursor solution in the first beaker. This combined solution now in the first beaker is stirred for 15 minutes at 300 RPM, after which it is dried at 120 °C in air for 24 hours. After drying, the material is crushed in a mortar and pestle. To carburize the sample, 1 g of crushed and dried material is added to a crucible. The sample is heated at a ramp rate of 15 °C/min to a hold temperature of ___ °C for ____ hr under 30 ccm of ___ gas. After carburization, the sample is cooled under 30 ccm of N2 gas until the tube furnace reads below 30 °C. The sample is passivated under 30 ccm of 1% O2/N2 gas for 2 hours

Timeline:

- May 18-19, 2026

  - Synthesis/carburization - check for difference in drying time (3 hrs) – Matt is also attempting to reproduce this (index M14)

    - Not enough liquid to dissolve sucrose – emailed Eva, also moved forward

  - Finish labeling of initial Mo dataset using simple systematic refinement approach

  - Finish BOICL loop:

    - Setup system message

    - Ensure correct objective function value extraction:

      - Feed in true labels with sigma (ucty.)

      - Ask only for phase composition values

      - If using reasoning model, log reasoning tokens

    - Consider running two regression tasks, one using GPT4o and one using Claude Opus for LLM selection. (consider using OCM and Marc’s synthetic dataset)

  - Check and apply BOICL loop using Marc’s synthetic data

- May 19-28, 2026

  - Start loop T1 (higher priority):

    - 3 Hr 20 min- synthesis (mixing and drying)

    - Carburization times will vary from .5 - 20 hr hold times – if we can do 2 in a day we will (send out for XRD asap)

  - Drop off T1 samples to Bill

  - Start loop T2 between xrd characterization

- May 20-29, 2026

  - Write paper

    - finish synthetic data sets / work on figures

      - Fig: BOICL-GSAS loop

      - Fig: confirming the simple systematic refinement steps make sense

      - Fig: Showing results from synthetic dataset (consider including regression tasks and reasoning token outputs)

      - Fig: Results from all trajectories